Basic Semiconductors

(Properties & Growth)

-	used for most solid state devices

-	silicon (and others)

Solid state device - a component whose operation depends on the control of electrical or magnetic phenomena in solids, such as a transistor, diode, or ferrite.

- could include glass lasers

We will concentrate on semiconductor devices.

What distinguishes semiconductors?

-	resistance/resistivity

-	crystaline structure

The resistance of a bar of material with dimensions L, W, t and resistivity r is:

W

R=ρLWt

t

L

metals: r < 10-3W-cm

insulators: r>102W-cm

semiconductors: 10-3W-cm < r < 102W-cm

Three types of solids, classified according to atomic arrangement: (a) crystalline and (b) amorphous materials are illustrated by microscopic views of the atoms, whereas (c) polycrystalline structure is illustrated by a more macroscopic view of adjacent single-crystalline regions, such as (a)

(a) Crystalline		(b) Amorphous		(c) Polycrystalline

Semiconductors are found in columns II-VI of the periodic table.  Why is silicon so popular if there are so many to choose from?

6

C

12			13			14			15			16

Mg		   Al		   Si		   P		   S

30			31			32			33			34

Zn		   Ga		   Ge		   As		   Se

48			49			50			51			52

Cd		   In		   Sn		   Sb		   Te

elemental semiconductors:   Si, Ge

compound semiconductors:   GaAs, InP

ternary semiconductors:   AlGaAs, HgCdTe

quaternary semiconductors:   InGaAsP, InGaAlP

Common semiconductor materials: (a) the portion of the periodic table where semiconductors occur; (b) elemental and compound semiconductors.

(a)		II			III			IV			V			VI

B			C

Al			Si			P			S

Zn			Ga			Ge			As			Se

Cd			In						Sb			Te

(b)

Elemental		IV Compounds		Binary III-V     Binary II-VI

compounds	compounds

Si				SiC					AlP				ZnS

Ge				SiGe				AlAs			ZnSe

AlSb			ZnTe

GaP			CdS

GaAs			CdSe

GaSb			CdTe

InP

InAs

InSb

Some characteristics of semiconductors

1)	melting temperature

2)	relative abundance/cost

3)	band gap (light generation/absorption)

4)	ease of doping

5)	ease of growth

6)	ease of processing

7)	performance

Crystal Lattices

· An ideal crystalline solid is periodic and is referred to as “single crystal”

· The periodic arrangement is called the lattice.

· A unit cell is a volume that is repeated throughout the crystal.

A two-dimensional lattice showing translation of a unit cell by 	r + 3a + 2b.

D’		E’

O’

F’

D		E

b			r

a	F

· A unit cell need not be “primitive” (the smallest possible unit cell).

In Fig. 1.2 (p.6),  a and bare called basis vectors (defined by the sides of the unit cell).

· Points within the lattice are indistinguishable if the vector r  between the points is givin by

r=pa+qb+sc			(1.1)

p, q, s   intergers

(·  future:  we will find that the lattice dimensions are involved in the allowed energies of the electrons in the crystal.)

Fig 1.3  Unit cells for three types of cubic lattice structures.

Fig 1-4 Packing of hard spheres in an fcc lattice.

·  The dimensions a,  b,  and  c  are called lattice constants.

Packing factor (fcc)  (Example 1-1)

·  Assume nearest neighbors touch (maximum packing)

a/2

c

a/2

a

a22+a22=c2=2a24⇒c=122a

The radius of the spheres =  24a

atoms/cell:

each corner contributes 1/8

(8 corners) Þ  1 sphere

each face contributes 1/2

(6 faces) Þ  3 spheres

Packing factor = (# of spheres/cell) Vsphere

Vunit cell

=443P24a3a3=423P2343a3a3=P233⋅4P26=0.7404...=74%

Planes and Directions

· We can define a plane in the crystal lattice with 3 integers:

1.  find the intercepts of the plane in terms of integral multiples of the basis vectors

[(Fig 1-5Þ2a, 4b, 1c]

2.  take the reciprocal of the integers and reduce to smallest set of integers h, k, l 										12,14,1→2,1,4

3.  label the plane (h k l)	214

· h,k,l are known as Miller Indices

· if the intercept is negative, the minus  sign is written above the indice:

hkl	[pronounced “h, k-bar, l”]

Fig 1.5 A (214) crystal plane.

Fig. 1-6	Equivalence of the cubic faces (100 planes) by 				rotation of the unit cell within the cubic lattice.

Directions in a crystal

·	direction is expressed as a set of 3 integers

·	the 3 integers represent the vector 	components of the direction along the 	crystalographic axis a,b,c

Fig. 1-7	Crystal directions in the cubic lattice

Fig. 1-8	Diamond lattice structure: (a) a unit cell of the 					diamond lattice constructed by placing atoms 1/4, 				1/4, 1/4 from each atom in an fcc; (b) top view (along) 				of an extended diamond lattice.  The colored circles 				indicate one fcc sublattice and the black circles 					indicate the interpenetrating fcc.

(a)									(b)

(special facts, cont’d)

A group of equivalent planes is referred to by braces:

010,001,100,010,001º100

Miller Notation Summary

convention					meaning

(hkl)							crystal plane

{hkl}							equivalent planes

[hkl]							crystal directions

<hkl>							equivalent directions

The Diamond Lattice

·	basic lattice for many elements (Si, Ge)

·	basic lattice for many compound 	semiconductors (GaAs, InP...)

In compound semiconductors that have the “diamond lattice”, one element (Ga or Zn) is placed on one fcc lattice and the other element (As or S) is placed on the other fcc lattice.

Fig. 1

1/2

1/2

0

1/2

0

1/4

3/4

1/4

0

0

0

3/4

As or S

Ga or Zn

1/2

Fig.1	Atomic positions in the unit cell of the diamond structure projected on a cube face.  Fractions denote height.  The points at 0 & 1/2 are on one set of fcc lattices (As or Zn), while the points 1/4 and 3/4 are on another set of fcc lattices (Ga or Zn) [known as zinc blende structure]

Example:  Find the number of Si atoms/cm2 on the (100) surface of a Si wafer.

a

a=5.43 A°

(room temperature)

For an area of a2, there are:

4 corner atoms which each contribute 1/4

1 center atom which is not shared

1+1=2 atoms/cell

Þ	      2      =   2       =      6.783...X 1014 atoms/cm2

(5.43 A°)2	(5.43 X 10-8cm)2

on (100) plane

Another Example:  Find the number of silcon atoms on the (110) plane:

Figure 21  Miller indices of some important planes in a cubic crystal.  The plane (200) is parallel to (100), but it divides the unit cube in two equal parts.

Fig 1.9	Diamond lattice unit cell, showing the 				four nearest neighbor structure.

In, Al, Ga  and column III elements and all go on the same sublattice.

As and P are column V elements and all go on the other sublattice.

In AlX Ga1-X As, with x=0.3,

Þ 30% of the column III sites are Al,

70% are Ga.

In InX Ga1-X AsY P1-Y  with x=0.47, y=0.25

Þ	47% of the column III sites are In

53% are Ga

Þ	25% of the column V sites are As

75% are P

Properties of Semiconductor Materials

Example 1.3		Calculate the density of Si from the lattice constant, atomic weight, and Avogadro’s number.  Recall: Avogadro’s number (6.02 X 1023) is the number of molecules/atoms in a gram molecular wight of a substance.

lattice constant = a = 5.43 X 10-8cm

how many Si atoms in the diamond cell?

8 corner atoms X (1/8) = 1

6 face atoms X (1/2) = 3

+ 4 interior atoms = 4			8 atoms/unit cell

(see Fig. 1-8 p. 25)

# of atoms   =    8     =           	8                      =

cm3			a3			(5.43 X 10-8 cm)3

=        8         =  4.996... X 1022 atoms/cm3

1.60 X 10-22

density = ofatomscm2ofgramsmoleofatomsmole=

gramscm3=4.996X1022atomscm328.1gmole6.02X1023=

=2.332gcm3

Comments on crystal planes

·	mechanical, electrical, chemical and optical properties depend on crystal orientation.

·	crystals can be cleaved along atomic planes Þ very flat, smooth surfaces

·	mirror facets for semiconductor lasers

·	wet chemical etchants etch along crystal planes

Electronic Grade Silicon:

1.

sand (SiO2)		SiC(solid) + SiO2(solid)

coal, wood 	® Si(liquid) + SiO(gas) + CO(gas)

chips, ...

heat

The liquid Si solidifies (~98% pure) (called metalurgical grade silicon -- impurities of ~few thousand ppm

2.	The solid silicon is pulverized and subjected to HCl gas:

Si(solid) + 3HCl(gas) ® SiHCl3(gas) + H2(gas)

SiHCl3 is called trichlorsilane.

3.	EGS is prepared from SiHCl3:

2SiHCl3(gas) + 2H2(gas) ® 2Si(solid) + 6HCl(gas)

result: high purity (a few ppm) EGS

(In 1998, ~95% of all semiconductor devices produced were silicon devices)

Methods to produce Single Crystals

·		Horizontal Bridgeman

·		Czochralski

·		Floating Zone

Fig 1-11	Crystal growing from the melt in a crucible: (a) 	solidification 			from one end of the melt (horizontal Bridgman method); (b) 			melting and solidification in a moving zone.

Fig. 1-2	Pulling of a Si crystal from the melt (Czochralski 							method): (a) schematic diagram of the crstal growth process.

Fig. 1-14	Floating-zone crystal growth: (a) schematic 						diagram of the growth process.

The Distribution Coefficent

For any material, there is a different afffinity for impurities for the liquid phase and the solid phase.  This characteristic is described by the distribution coefficent kd.

kd = cS/cL

cS = impurity concentration in the solid

cL = impurity concentration in the liquid

kd = f(material, impurity, temperature)

Example:	  if kd=1/2, there are twice the impurities in the liquid as in the solid.

Example 1-4  Find the concentration of phosphorous (P) atoms in the melt to obtain Si doped with 1016 atoms/cm3 (Czochralski growth)

kd = 0.35 for P in S

kd=cScL=1016atomscm30.35=2.86X1016atomscm3

b)	how many grams of P should be added if the inital load in the crucible is 5 kg of Si?

density of Si = 2.33g/cm3

the volume of Si in the melt is

5000g2.3gcm3=2145.9cm3

In the total melt volume, we want 2.86X1016 atoms/cm3.

The number of atoms is

2.86X1016atomscm3VSi+VP

but VP << VSi, so VC » Vsi

P atoms =	2.86X1016atomscm32145.0cm3=6.137X1019

637X1019atoms´31gmole6.023´1023atomsmole=3.159´10−3g=3.16mg