Boundary conditions:

at x=¥, dp=0⇒c1=0

at x=0, dp=Dp⇒c2=Dp

so	dpx=Dpe−xLp						(16)(4-36)

· dpx⇒Jdiff=-qDpdpxdx

· px=p0+Dpe−xLp

⇒dpxdx=-DpLpe−xLp

Jpdiff=qDpLpDpe−xLp=qDpLpdpx		(17)(4-40)

· the diffusion current is proportional to the excess concentration dpx

The Haynes-Shockley Experiment

· 1951, Bell Labs

· independent measurement of minority carrier mobility (m) and diffusion coefficient (D)

· basic principles

-e field applied to semiconductor bar

-narrow pulse, high concentration of minority carriers generated

-pulse drifts due to e (time to drift a fixed distance Þ mobility

-pulse spreads due to diffusion (Þ diffusion coefficient)

In Fig. 4-18 (n-type material n0 >> p0)

-pulse of holes generated at t=0

-n=n0+dn»n0		dn<<n0

-p=p0+dp			dp>>p0

-pulse of holes drift in e direction

-pulse monitored at x = L; drift velocity Vd is

Vd=Ltd							(18)(4-41)

mp=Vde=Ltde						(19)(4-42)

Haynes-Shockley ® minority carrier m

Hall Effect ® majority carrier m

H-S Pulse Spreading

· consider diffusion without drift or recombination

· Eq (13b) or (4-33b) (p. 418):

¶dpx,t¶t=Dp¶2dpx,t¶x2					(19)(4-43)

if dpx=0,t=0=Dp

the solution to (19) is

dpx,t=Dp2pDpte−x24Dpt			(20)(4-44)

check:   ¶dp¶t=¶¶tc1t−12e−x24Dpt

=c1t−12¶¶teux,t−12c1t−32eux,t

where c1=Dp2pDp , now		¶¶teu=eu¶u¶t

u=−x2t−14Dp⇒dudt=+x2t−24Dp

so	¶dpx,t¶t=c1t−12eux2t−24Dp−12c1t−32eu		(A)

what does ¶2¶x2 give us?

¶2dpx,t¶x2=¶¶x¶¶xc1t−12e−x24Dpt

¶¶xc1t−12eu=c1t−12eududx

where		u=−x24Dpt⇒dudx=−2x4Dpt

so		¶2dpx,t¶x2=¶¶x−24Dptc1t−12xeu

=−2c14Dpt32¶¶xxeu

since		¶¶xxeu=x¶¶xeu+eu=xeu−2x4Dpt+eu

we have

¶2dpx,t¶x2=−2c14Dpt32−2x24Dpt+1eu					(B)

simplifying (B)

¶2dpx,t¶x2=C1Dpt32x24Dpt−12eu					( C)

and rearranging (A):

¶dpx,t¶t=c1t32x24Dpt−12eu

we verify that

¶dpx,t¶t=Dp¶2dpx,t¶x2

Þ the gaussian distribution given by (20) is a solution to (19) [(4-43)]

considering (20):

dpx,t=Dp2pDpte−x24Dpt

Note that

· the amplitude decreases w/ time

· the pulse width increased w/ time

· pulse width = full width @ 1/e pts.

· for a fixed peak height dp , the pulse width Dx can be found

e−1dp=dpe−Dx24Dptd				(21)(4-45)

where td is the time corresponding to the pulse spread Dx

· (21) Þ Dx224Dptd=1 , or Dp=Dx216td			(22)(4-46)

If we use the circuit in Fig. 4-20, we can relate the spatial pulse width Dx to the voltage pulse V(t) seen on the oscilloscope by

Dx=DtVd=DtLtd							(23)(4-47)

Example 4-6	n-type Ge is used in a Haynes-Schockley experiment.  The length of the Ge bar is 1 cm, the probes are spaced 0.95 cm apart.

· battery voltage is 2.0 V

· td = 0.25 ms

· pulse width Dt (oscilloscope) = 117 ms

Find mp and Dp (and check agreement w/ the Einstein relations)

mp=Vde

e=VL0=2Vcm

Vd=Ltd=0.95cm0.25´10−3sec=3800cm/sec

mp=3800cm/sec2Vcm=1900cm2Vs

Dp=Dx216td

Dx=DtVd=117´10−6s3800cms=

=0.446cm

so

Dp=0.446cm2160.25´10−3s=49.4cm2s

Dpmp=49.4cm2s1900cm2V⋅s=0.026V

kTq=.0259eVe=.0259V

alternatively, in Joules

k=1.38´10−23J°K

kT=1.38´10−23J°K300°K=4.14´10−21J

kTq=4.14´10−21J1.60´10−19C=0.0258J/C

recall:  power = watt = J/s = IV Þ amp×volts

Js=Csvolt⇒J=C⋅volt ,

so		kTq=0.0258V

Quasi Fermi Levels and Current Density

at equilibrium

dEFdxº0

(EF is only defined for equilibrium)

recall, at equilibrium:

n0=nieEF−EikT								(3-25a)

p0=nieEi−EFkT								(3-25b)

and for steady-state conditions:

n=nieFn−EikT									(4-15a)

p=nieEi−FpkT									(4-15b)

we found that current density is given by [4-23a,4-23b]

Jnx=qmnnxex+qDndnxdx

Jp=qmppxex−qDpdpxdx

If the electron concentration is varying, we have

nx=nieFnx−EixkT=nieux

so	dnxdx=nieuxdudx						(24)(4-49)

=nxkTdFnxdx−dEixdx

so Jn becomes

Jnx=qmnnxex+qDnnxkTdFndx−dEidx

since Dm=kTq⇒qDkT=m ,  so

Jnx=qmnnxex+mnnxdFndx−dEidx	(26)(4-50)

However, by Eq. (4-26), we related e(x) to band bending by (p. 403)

ex=1qdEidx									(4-26)

so	Jnx=qmnnx1qdEidx+mnnxdFndx−mnnxdEidx

with the result:

Jnx=mnnxdFndx					(27a)(4-51)

similarly for holes

Jpx=mppxdFpdx					(27b)

- The process of drift and diffusion are proportional to the slope of the quasi-Fermi levels

By analogy w/ Ohms Law

J=se

s=qmnnx,  electrons

s=qmppx,  holes

we can write (27a,b) as

Jnx=qmnnxdFnÁqdx=snxdFnqdx

(28a)(4-52a)

Jpx=qmppxdFpqdx=spxdFpqdx

(28b)(4-53b)

Example (proble 4.7, text)

Find an expression for Fp(x) for an exponential hole distribution (Fig 4.17, p420):		(for p(x)>>p0)

dpx=Dpe−xLp

for					dpx>>p0

px»Dpe−xLp=nieEi−FpkT

Ei−Fp=kTlnDpe−xLpni

Ei−Fp=kTlnDpni−xLp

the band diagram looks like:

Silicon: ni = 1.5 X 1010

Dp=1014

Lp=Dptp12=12.5´10−612=0.0035cm

Ei−Fp=.025911.1−x0.0035cm		Dp = 12.5 cm2/s

tp = 1ms

Problem 1   HW #10

Compensation problem:

- p. 302 explains why EF = Ei

- are the dopants fully ionized?

For ND+=1017, NA−=0,  ND+ND=0.96

for ND+=NA−⇒EF=Ei ,

ND+ND=1 , (actually @1−6´10−9

and		NA−NA=1  1−2´10−8

- high resistivity (experimentally)

- ?

At 300°K , Ev º 0

Ec=1.11eV

Ei=Eg2−0.0153eV=0.5397eV

Eg2=0.555eV

EFND=1017cm3=Ei+0.407eV=0.9467eV

(As) ED=EC−0.054=1.046eV

EC-ED

- EA=.045

kT=0.0258eV@300°K

ND+ND=11+gDeEF−EDkT

for  EF=0.9467eVND+=1017,NA−=0

ND+ND=11+2e0.9467−1.0460.02586

ND+ND=11+20.02149=0.959

for EF=0.9467 ND+=1017,NA−=0

for ND+=NA−⇒EF=Ei=0.5397eV

ND+ND=11+2e0.5397−1.0460.02586

=11+2e−19.5785=11+6´10−9

fE=11+eE−EFkT

for an electron at E = EA = 0.045eV

EF = Ei = 0.5397eV:

fAEA=11+4e0.045−0.5397kT

=11+4e−19.12993=11+2´10−8

at EF=Ei ,

the probability of a hole at ED@1⇒ fully ionized:  Nd+=Nd

the probability of an electron at EA@1⇒ fully ionized:  NA−=NA

- so what happens?

Donors:

Acceptors:

2B2O3+3SiÛ4B+3SiO2

P-N Junction Diodes

-step junction

· sharp interface between n-p

· obtained by epitaxial growth, alloying

· simplest to analyze

-graded junction

· obtained by diffusion, implantation

Contact Potential and Current Flow

-equilibrium Þ net current flow = 0

-consider two separate p & n region – and bring together at t=0:

· conduction band electrons are free to move (diffuse), but the donor atoms are fixed

· valence band holes also free to move, but acceptor atoms fixed

Þ space charge region due to free carrier diffusion

® space charge results in e field

® e field causes drift currents that oppose the diffusion currents

JTOTAL=Jpdrift+Jpdifffusion+Jndrift

+Jndiffusion=0

(for equilibrium)